## Slide 1: Morphological profiling of drug particles: influence of shape and surface architecture on critical quality attributes
Dr Sopan N. Nangare
Assistant Professor
Department of Pharmaceutics,
Krishna Institute of Pharmacy,
Krishna Vishwa Vidyapeeth (Deemed to be University), Karad, Maharashtra, India
Resource Person

## Slide 2: Learning outcomes
After completing this session, students will be able to
Define particle morphology and explain its components, including shape, size, surface texture, and surface energy
Differentiate between particle shapes and describe their formation during crystallization and processing
Explain how surface architecture analyze the relationship between morphology and critical quality attributes (CQAs) such as:
Dissolution rate
Correlate morphological changes with manufacturing processes such as milling, granulation, spray drying, and crystallization
Assess regulatory considerations related to morphology as part of pharmaceutical quality by design (QBD)

## Slide 3: Contents
Introduction to particle morphology
01
Fundamentals of particle shape and size
02
Surface architecture of drug particles
03
Morphology and critical quality attributes (CQAs)
04
Analytical techniques for morphological profiling
05
Manufacturing processes and morphology control
06

## Slide 4: Contents
Regulatory and quality considerations
07
Case studies
08
Conclusion
09

## Slide 5: Introduction to particle morphology
Definition of particle morphology
  Importance in pharmaceutical sciences
  Role in drug development and manufacturing
  Connection to critical quality attributes (CQAs)

## Slide 6: Definition and Significance
Particle morphology includes shape, size, and surface structure
  Determines powder behavior and processing performance
  Influences dissolution and bioavailability
  Essential for quality by design (QbD) approach

## Slide 7: Overview of solid-state properties
Crystallinity and amorphous nature
  Polymorphism and crystal lattice structure
  Surface energy and wettability
  Mechanical properties of particles

## Slide 8: Surface and structural characteristics
Surface roughness and porosity
  Internal microstructure
  Surface defects and imperfections
  Impact on stability and degradation

## Slide 9: Morphology as determinant of drug performance
Affects dissolution rate
  Controls flowability and compressibility
  Impacts content uniformity
  Influences stability and shelf-life

## Slide 10: Fundamentals of particle shape and size
Importance of particle geometry
  Relation to manufacturing processes
  Influence on powder mechanics
  Measurement techniques overview

## Slide 11: Geometric descriptors
Aspect ratio (length/width relationship)
  Circularity (degree of roundness)
  Sphericity (similarity to a sphere)
  Shape factor and elongation index

## Slide 12: Crystal habit and polymorphism
Crystal habit: external crystal shape
  Polymorphism: multiple crystal forms
  Impact on solubility and dissolution
  Examples in pharmaceutical compounds

## Slide 13: Influence of crystallization conditions
Effect of solvent selection
  Temperature and cooling rate
  Supersaturation levels
  Presence of additives and impurities

## Slide 14: Control strategies in particle engineering
Optimization of crystallization parameters
  Use of spray drying and milling
  Monitoring via process analytical technology (PAT)
  Ensuring consistent particle quality

## Slide 15: Surface architecture of drug particles
Definition of surface architecture
  Importance in pharmaceutical performance
  Relation to particle engineering
  Impact on critical quality attributes (CQAs)

## Slide 16: Surface roughness and texture
Definition of surface roughness
  Micro- and nano-scale surface irregularities
  Influence on interparticle friction
  Effect on dissolution and adhesion properties

## Slide 17: Porosity and internal structure
Definition of porosity (open vs closed pores)
  Internal microstructure characteristics
  Influence on surface area and drug release
  Role in moisture uptake and stability

## Slide 18: Surface energy and wettability
Concept of surface free energy
  Hydrophilic vs hydrophobic surfaces
  Contact angle and wetting behavior
  Influence on dissolution and bioavailability

## Slide 19: Amorphous vs crystalline surfaces
Structural differences between amorphous and crystalline forms
  Higher energy state of amorphous materials
  Impact on solubility and stability
  Risk of recrystallization during storage

## Slide 20: Morphology and critical quality attributes (CQAs)
Relationship between particle morphology and product quality
  Impact on drug performance and manufacturability
  Key CQAs influenced by morphology
  Regulatory relevance in pharmaceutical development

## Slide 21: 4.1 Dissolution and bioavailability
Surface area directly influences dissolution rate
  Smaller particles → higher surface area → faster dissolution
  Morphology affects diffusion layer formation
  Critical for oral bioavailability

## Slide 22: Surface area, wettability, and porosity
High surface area enhances drug-solvent interaction
  Wettability governs liquid penetration
  Porous particles increase effective surface area
  Hydrophobic surfaces may delay dissolution

## Slide 23: Case example: carbamazepine polymorphs
Different polymorphs exhibit distinct crystal packing
  Variation in solubility and dissolution rate
  Metastable forms may dissolve faster
  Polymorphic control is essential for consistent bioavailability

## Slide 24: 4.2 Flowability and powder handling
Particle shape influences flow properties
  Spherical particles flow better than needle-shaped ones
  Surface roughness increases friction
  Essential for large-scale manufacturing

## Slide 25: Cohesion and electrostatic interactions
Fine particles exhibit stronger cohesive forces
  Electrostatic charge affects powder handling
  Humidity influences interparticle attraction
  Impacts die filling and uniformity

## Slide 26: Impact on capsule filling and tablet compression
Poor flow causes weight variation
  Irregular particles may bridge in hoppers
  Affects content uniformity
  Critical for dosage accuracy

## Slide 27: 4.3 Compressibility and compactibility
Ability of powder to reduce volume under pressure
  Dependent on particle shape and size distribution
  Influences tablet hardness and friability
  Important for direct compression formulations

## Slide 28: Fragmentation vs plastic deformation
Brittle materials undergo fragmentation
  Ductile materials deform plastically
  Fragmentation increases bonding surface area
  Plastic deformation enhances interparticle bonding

## Slide 29: Mechanical interlocking of irregular particles
Irregular shapes promote mechanical interlocking
  Enhances tablet strength
  May reduce flowability
  Balance required during formulation design

## Slide 30: 4.4 Stability and Degradation
Surface morphology influences chemical stability
  High-energy surfaces prone to degradation
  Exposure to light, oxygen, and moisture
  Surface defects act as reactive sites

## Slide 31: Surface-mediated oxidation and hydrolysis
Surface area increases exposure to reactive species
  Amorphous regions more reactive than crystalline
  Moisture accelerates hydrolytic degradation
  Protective coatings may improve stability

## Slide 32: Example: hygroscopicity in aspirin
Moisture uptake varies with particle morphology
  Hydrolysis forms salicylic acid
  Surface area influences degradation rate
  Proper storage minimizes stability issues

## Slide 33: Analytical techniques for morphological profiling
Importance of particle characterization
  Link between morphology and performance
  Role in quality by design (QbD)
  Overview of analytical approaches

## Slide 34: Microscopy methods overview
Direct visualization of particle morphology
  Surface and structural examination
  Micro to nano-scale analysis
  Qualitative and quantitative assessment

## Slide 35: Scanning electron microscopy (SEM)
High-resolution surface imaging
  Topographical and morphological details
  Useful for irregular and porous particles
  Requires conductive coating for non-metals

## Slide 36: Applications of SEM in pharmaceuticals
Crystal habit identification
  Surface roughness evaluation
  Detection of agglomeration
  Pre- and post-processing comparison

## Slide 37: Atomic force microscopy (AFM)
Nano-scale surface characterization
  Measures surface roughness quantitatively
  Operates in contact or tapping mode
  Useful for soft and amorphous materials

## Slide 38: Optical microscopy
Basic particle shape observation
  Polymorph differentiation (limited)
  Cost-effective and simple method
  Used for routine quality control

## Slide 39: Particle size analysis techniques
Critical for dissolution and flowability
  Determines size distribution profile
  Affects bioavailability
  Supports formulation development

## Slide 40: Laser diffraction
Measures particle size distribution
  Based on light scattering principles
  Suitable for wide size range
  Rapid and reproducible method

## Slide 41: Dynamic light scattering (DLS)
Used for nano-sized particles
  Measures brownian motion
  Determines hydrodynamic diameter
  Common in nanosuspensions

## Slide 42: Surface and solid-state characterization
BET surface area analysis for porosity
  Contact angle for wettability
  XRD for crystallinity and polymorphism
  DSC for thermal transitions

## Slide 43: Manufacturing processes and morphology control
Importance of controlling particle properties
  Impact on critical quality attributes
  Process-structure relationship
  Role in scalable production

## Slide 44: Crystallization parameters overview
Primary method of particle formation
  Controls crystal size and habit
  Influences polymorphic form
  Critical for drug substance quality

## Slide 45: Effect of temperature
Cooling rate influences crystal size
  Rapid cooling → smaller crystals
  Slow cooling → larger, well-formed crystals
  Affects purity and morphology

## Slide 46: Effect of solvent selection
Solvent-solute interactions affect habit
  Polarity influences crystal growth
  Solvent may stabilize polymorphs
  Impacts surface energy

## Slide 47: Supersaturation control
Driving force for nucleation
  High supersaturation → rapid nucleation
  Low supersaturation → controlled growth
  Determines size distribution

## Slide 48: Spray drying
Produces amorphous or spherical particles
  Rapid solvent evaporation
  Enhances dissolution rate
  Used for solid dispersions

## Slide 49: Freeze drying (lyophilization)
Removes solvent via sublimation
  Creates porous structures
  Improves reconstitution properties
  Common for biologics

## Slide 50: Milling and micronization
Reduces particle size mechanically
  Increases surface area
  May induce amorphization
  Impacts flow and stability

## Slide 51: Granulation techniques
Wet and dry granulation methods
  Improves flowability
  Enhances compressibility
  Reduces dust and segregation

## Slide 52: Process analytical technology (PAT) tools
Real-time monitoring of processes
  Near-infrared spectroscopy (NIR)
  In-line particle size measurement
  Ensures consistent morphology control

## Slide 53: Regulatory and quality considerations
Role of morphology in pharmaceutical quality
  Regulatory expectations for solid dosage forms
  Impact on safety, efficacy, and consistency
  Integration into quality systems

## Slide 54: Morphology within quality by design (QbD)
Scientific understanding of material attributes
  Design space for particle properties
  Link between CPPs and CQAs
  Risk-based development approach

## Slide 55: Morphology as a critical quality attribute (CQA)
Definition of CQA in pharmaceutical development
  Influence on dissolution and bioavailability
  Effect on manufacturability and stability
  Need for scientific justification and control

## Slide 56: ICH guidelines relevance
ICH Q8 - pharmaceutical development
  ICH Q9 - quality risk management
  ICH Q10 - pharmaceutical quality system
  Supports lifecycle management strategy

## Slide 57: Control strategies and risk assessment
Raw material and polymorph control
  Process parameter monitoring
  Failure mode and effects nalysis (FMEA)
  Continuous process verification

## Slide 58: Case studies in morphological impact
Real-world examples of morphology influence
  Polymorphism and bioavailability changes
  Manufacturing challenges due to shape
  Importance of process control

## Slide 59: Polymorphic transformation and bioavailability
Different crystal forms show varied solubility
  Metastable forms may enhance dissolution
  Risk of transformation during storage
  Impact on therapeutic performance

## Slide 60: Needle-shaped crystals and tablet defects
Poor flow due to high aspect ratio
  Increased interparticle friction
  Weight variation during compression
  Potential capping and lamination defects

## Slide 61: Spray-dried amorphous solid dispersions
Amorphous form improves solubility
  Higher surface energy enhances dissolution
  Risk of recrystallization
  Requires stability monitoring

## Slide 62: Lessons from case studies
Morphology directly affects CQAs
  Importance of analytical monitoring
  Need for robust formulation strategy
  Regulatory implications of polymorphism

## Slide 63: Conclusion: morphology-performance relationship
Strong link between particle properties and CQAs
  Shape and surface affect drug release
  Manufacturing depends on particle behavior
  Integrated control strategy required

## Slide 64: Importance in pharmaceutical development
Ensures product consistency
  Improves manufacturability
  Enhances therapeutic effectiveness
  Supports regulatory approval

## Slide 65: Future trends in particle engineering
Advanced crystal engineering techniques
  Nano- and micro-particle design
  AI-driven process optimization
  Continuous manufacturing approaches

## Slide 66: Emerging technologies
In-line morphological monitoring tools
  Advanced microscopy techniques
  Improved solid dispersion systems
  Smart formulation strategies

## Slide 67: Final summary
Morphology is a critical determinant of drug quality
  Requires multidisciplinary understanding
  Controlled through QbD and PAT tools
  Essential for modern pharmaceutical innovation